## Slide 1
Strength Analysis
ENCH 5910 / ENCH 7997
TMOS AEROGEL
Syed Mohammed Tareq
Department of Computational Science and Engineering

## Slide 2
Sample without seal
Sample with Seal, vacuum time 10 secs (Single and Double layer)
Sample with Seal, vacuum time 20 secs (Single and Double layer)
Sample with Seal, vacuum time 40 secs (Single and Double layer)
SCOPE

## Slide 3
Load vs Extension
SCOPE

## Slide 4
Schematic Image
Universal Testing Machine

## Slide 5
Working principle & Key equations & Applications
Universal Testing Machine

## Slide 6
Data examples
Universal Testing Machine

## Slide 7
Load vs Extension
Comments:
Load and extension is correlated.
Small load with small strain may give more stress.

## Slide 8
Stress vs Strain

## Slide 9
Stress vs Strain
Comments:
Stress with vacuum time (VT) 40 second and double layer seems to be higher.
One sample data of VT20 with Double (D) layer is corrupted.
Value is matching with the article shown below
Refs: https://pubs.acs.org/doi/full/10.1021/acs.jpcb.7b03184
Key questions
Place, side by side to compare

## Slide 10
Sample cracked with a load 1.45 N | 
Future Plan
Vacuum sealing using fresh sample with various options and test the change in strength
Completion of UVvisNIR analysis prior to strength test
Start of manuscript on vacuum aerogel

## Slide 11
Conclusion
Better result may be found from the samples dried with 100 % EtOH.